## Slide 1: Design of Silicon Photonic Bragg Grating Devices Vancouver, BC, Canada 25 May 2020
Mustafa Hammood,
The University of British Columbia, Vancouver

## Slide 2: Outline
  Bragg gratings:
    Motivation and application
    Theoretical approach: Transfer-Matrix Method (TMM)
    Simulation: Lumerical EME
    Simulation: Lumerical 3D/2D FDTD
    Simulation: Lumerical FDTD Band-structure
    Theoretical approach: Coupled-mode theory (CMT)
      Coupling coefficient (Kappa)
  Contra-directional couplers:
    Theoretical approach
    Simulation: Lumerical EME
    Simulation + Theory: Coupled-mode theory + Transfer-Matrix Method
    Compact model generation and full-simulation flow

## Slide 3: Bragg Gratings: References
  Bragg gratings and contra-directional couplers tutorial: https://www.youtube.com/watch?v=jr3NcJsKvTI
  SiEPIC PDK KLayout integration of Bragg Gratings: https://www.youtube.com/watch?v=h2MOOhsuYpA
  SiEPIC PDK KLayout integration of Contra-directional couplers: https://www.youtube.com/watch?v=aqocwLcqC0s
  and
  https://www.youtube.com/watch?v=-vWspXuu8I0

## Slide 4: Bragg Gratings: Transfer-Matrix Method

## Slide 5: Bragg Gratings: Transfer-Matrix Method
  Available: https://github.com/mustafacc/SiEPIC_Photonics_Package/blob/master/SiEPIC_Photonics_Package/solvers_simulators/bragg_tmm/bragg_tmm.py
  Handy tool to quickly model phase-shifted Bragg gratings
  Inputs:
    Waveguides compact models (effective indices fits, n(λ) )
    Period
    Number of corrugations
    Perturbation size
  Advantages:
    Quick and simple
    Does not scale up with the length of the device
    Can simulate complex device profiles (apodized, chirped, etc.)
  Disadvantages:
    Must have data to fit the coupling coefficient profile vs perturbation size!

## Slide 6: Bragg Gratings: Transfer-Matrix Method
  Run bragg_tmm.py

## Slide 7: Bragg Gratings: EME
  Uses the EME method:
    Explained: https://apps.lumerical.com/pic_passive_bragg_full_device_simulation_with_eme.html
    Video tutorial: https://www.lumerical.com/support/video/waveguide-bragg-gratings-res.html
  Advantages:
    Does not need information other than the physical geometry of the device
    Relatively fast simulation time compared to FDTD
  Disadvantages:
    Simulation time scales up with the complexity of the profile
    Simulation time scales up with the number of simulation modes required to simulate the device
    Less accurate than FDTD simulations

## Slide 8: Bragg Gratings: EME
  How to:
    Download the scripts (Bragg_EME.zip) and open a blank MODE project
    With the new MODE project, load the script MAIN_EME.lsf
    Adjust the simulation parameters to your needs (wavelength range, polarization, mesh accuracy or leave as default)

## Slide 9: Bragg Gratings: EME
  How to:
    The script will plot the transmission and reflection spectra, and then extract the 3-dB bandwidth and central wavelength (for your future Kappa analysis).

## Slide 10: Bragg Gratings: EME
  How to:
    The script will plot the transmission and reflection spectra, and then extract the 3-dB bandwidth and central wavelength (for your future Kappa analysis).
Δλ
λo

## Slide 11: Bragg Gratings: EME
  EME simulations can be used to quickly perform parametric studies to understand the effects of specific parameters, i.e. the effects of changing the waveguide’s sidewall angle:
  Run applications -> dw_sweep -> MAIN_dw_sweep.lsf

## Slide 12: Bragg Gratings: EME
  The scripts will force specific settings to improve the simulation speed (e.g., force anti-symmetric boundary conditions when the user specifies the TE polarization) - therefore, if you care more about accuracy rather than speed, you might want to remove these settings from Bragg_simulate.lsf.

## Slide 13: Bragg Gratings: 3D/2D FDTD
  Uses FDTD solver:
    Simulating the full device length either in 2D FDTD or 3D FDTD
  Advantages:
    Accurate, if the simulation mesh and time were sufficiently large…
    Can be used to simulated complex apodization provide.
  Disadvantages:
    Very lengthy simulation time!

## Slide 14: Bragg Gratings: 3D/2D FDTD
  Open new FDTD project and load sample code MAIN_FDTD.lsf
  Input parameters:
    Device physical parameters
    Simulation parameters
  You can create an S-parameters sweep as well.
    You can use ports symmetry.
* There are rarely times you need to actually use 3D FDTD to simulate an entire length of a Bragg grating device. The example is added here for illustrating the inefficiency of the method relative to other methods.

## Slide 15: Bragg Gratings: FDTD Bloch Boundary
  Uses FDTD solver:
    Simulating one unit cell of a grating over an infinite length.
  Advantages:
    Relatively fast simulation with the most accurate results.
    Can be used to perform various parametric sweeps.
  Disadvantages:
    Cannot simulate the output spectra of advanced apodized devices (directly).
    Does not show the output spectra of the device
  More at:
    https://support.lumerical.com/hc/en-us/articles/360042304394-Bragg-Grating-Initial-Design-with-FDTD

## Slide 16: Bragg Gratings: FDTD Bloch Boundary
  Two examples provided under ‘Bandstructure’
    Script-based: run ‘MAIN_Bandstructure.lsf’ using FDTD script window with simulation and physical parameters. This is a “GUI”-less approach that will setup the simulation for you.
    Project-based: open “Bragg_bandstructure.fsp’ using FDTD and configure the simulation settings under “model” and physical settings under “Bragg” objects.
      Sample parametric sweeps were setup in this project as an example.

## Slide 17: Bragg Gratings: FDTD Bloch Boundary
  How to (method 1, script base):
    Download the scripts script_base.zip and open a blank FDTD project
    From FDTD, load the script MAIN_Bandstructure.lsf
    Adjust the simulation parameters to your needs (wavelength range, polarization, mesh accuracy

## Slide 18: Bragg Gratings: FDTD Bloch Boundary
  How to (method 1, script base):
    Adjust the device geometry, material, and process stack settings to your needs. Currently the default settings are set for SOI in mind, but it can be changed to any platform.

## Slide 19: Bragg Gratings: FDTD Bloch Boundary
  How to (method 1, script base):
    Run the script - given the current settings, it should run in under ~3 minutes.
    The script will extract the nulls bandwidth and central wavelength of the Bragg grating, which you can use to extract the Kappa (coupling coefficient) to be used in a coupled-mode theory model.
    You can visualize the results
Δλ
λo

## Slide 20: Bragg Gratings: FDTD Bloch Boundary
  How to (method 2, project base):
    Download the scripts project_base.zip and open Bragg_bandstructure.fsp this is an already setup simulation project.
    Right click on Model and edit the simulation settings and parameters to your requirements:

## Slide 21: Bragg Gratings: FDTD Bloch Boundary
  How to (method 2, project base):
    Right click on Bragg structure group and edit the device geometry, material, and process stack.

## Slide 22: Bragg Gratings: FDTD Bloch Boundary
  How to (method 2, project base):
    Run the simulation and let it run. Once the simulation is done you can right click on model and run the analysis to extract the coupling coefficient, bandwidth, and central wavelength of the Bragg grating.
Δλ
λo

## Slide 23: Bragg Gratings: FDTD Bloch Boundary
  How to (method 2, project base):
    I provided sample parametric sweeps in the optimization and sweeps tab that will help you understand the effects of each of the following parameters:
      Perturbation width
      Sidewall angle
      Bragg Period